TECHNICAL DATA SHEET

Product: Candle Lacquer 0218 – xxxxx

Type of Product:	Acrylic resin-based paint

Application:			Decorative coating for candles

Properties:			Fast-drying decorative paint

Solids:				31 % by weight		24 % by volume

Application:

Method:							Recommended viscosity:			Thinner:

Spraying							10 ± 2 sec. F4							0600-00213

Dipping							10 ± 2 sec. F4							0600-00213

Except:

Product 0218-06087 16 sec. ± 2 sec. F4

Product 0218-06213 16 sec. ± 2 sec. F4

STIR THE PRODUCT THOROUGHLY BEFORE AND DURING USE.

Drying:

Drying Time			Film thickness—dry

Dry to touch			4 minutes 20°C

Storage:				Frost-free

Shelf-life:			12 months in an unopened container

Cleaning:			Tools can be cleaned with Acetone for Candle lacquer 0600-00213

This information is based on our present state of knowledge and is intended to provide general notes on our products and their use.  Therefore, it should not be construed as guaranteeing specific properties of the product described or its suitability for a particular application.

Rungstedvej 75

DK-2960 Rungsted Kyst

T: +45 45 16 16 11 		F: +45 45 16 16 12		E: info@cawatec.com

www.cawatec.com