TECHNICAL DATA SHEET

Product: Candle Lacquer W 0556 – xxxxx

Type of Product:	Acrylic dispersion-based waterborne paint

Application:			Decorative coating for candles

Properties:			Fast-drying decorative paint

Solids:				26 % by weight		22 % by volume

Application:

Method:							Recommended viscosity:			Thinner:

Dipping							14-16 sec. F4							water

Except:

Product 0556-06086 25 sec. ± 2 sec. F4

STIR THE PRODUCT THOROUGHLY BEFORE AND DURING USE.

Drying:

Drying Time			Film thickness—dry

Dry to touch			30 minutes 20°C

Storage:				Frost-free

Shelf-life:			12 months in an unopened container

Cleaning:			Tools can be cleaned with water

This information is based on our present state of knowledge and is intended to provide general notes on our products and their use.  Therefore, it should not be construed as guaranteeing specific properties of the product described or its suitability for a particular application.

Rungstedvej 75

DK-2960 Rungsted Kyst

T: +45 45 16 16 11 		F: +45 45 16 16 12		E: info@cawatec.com

www.cawatec.com